## Slide 1
MOORING ROPES BASICS AND RECENT INNOVATIONS
Better Ideas in Action

## Slide 2
Introduction to Ropes

## Slide 3: Introduction to Polymers
A polymer is a large molecule of which is formed by repeated linking of the small molecules called “Monomers”.
More monomer molecules joined in units of long polymer.
Single Ethylene Molecule
Polyethylene
Addition of many single molecules

## Slide 4: Types of Polymers used for rope making
Polymer Materials used for rope making
High Density Polyethylene [HDPE]
Polypropylene [PP]
Polyester
Nylon
HMPE
Vectran
Aramids
Normal strength fibres
High Modulus fibres

## Slide 5: Properties of different types of materials
Sr. No. | Material properties | High Density Polyethylene | Polypropylene | Polyester | Nylon
1 | Tensile strength [N/mm2] | 0.20 - 0.40 N/mm² | 0.95 - 1.30 N/mm² | 2.5 N/mm² | 0.90 – 1.85 N/mm²
2 | Density [g/cm3] | 0.944 - 0.965 g/cm3 | 0.905 g/cm3 | 1.37 g/cm3 | 1.13 - 1.35/1.41 g/cm3
3 | Elongation at break [%] | 11-20% | 12-15% | 11-14% | 17-24%
4 | Abrasion resistance | Good | Moderate | Very Good | Moderate
5 | Shrinkage | Resistant to shrinkage | Resistant to shrinkage | Moderately resistant to shrinkage | Prone to shrinkage
6 | Water absorption | Does not absorb water | Does not absorb water | Absorbs some water | Absorbs most water
7 | UV Resistance | Good | Moderate | Very good | Good
8 | Floating properties | Floating | Floating | Sinking | Sinking
9 | Creep | High creep | Moderate creep | Low creep | Low creep
10 | Fatigue resistance in wet condition | Moderate | Good | Good | Low

## Slide 6: Rope Making process
Rope Making
Extrusion
Rope Making
Twisting
Strand making
01
02
03
04

## Slide 7: GTFL - Rope Making machines and facilities
3 STRAND ROPE MAKING M/C
8 STRAND ROPE MAKING M/C

## Slide 8: Rope Terminology
Filament/Fiber | Smallest individual element of continuous synthetic material used for rope making
Yarn | A number of fibers twisted together into a length as the first stage of rope making
Strand | A number of yarns twisted together in the opposite twist to the yarn
Twine | Thin cord of two or more strands of yarn
Cord | A number (usually three) strands twisted together with a circumference of 1"(25mm) or less
Rope | Cord of 1"(25mm) or more in circumference

## Slide 9: Rope Construction/Types of rope
3- Strand Rope.
4- Strand Rope.
8- Strand Rope.
12- Carrier Rope.
Braid On Braid Rope.

## Slide 10: 3 strand rope

## Slide 11: 8 strand rope

## Slide 12: 12 strand rope

## Slide 13: Braid on Braid rope

## Slide 14: Braided ropes with jacket
An offshoot of double braid is a rope in which a hollow braided or plaited core is used to carry the load, and a braided jacket is used to protect it from external abrasion.

## Slide 15: Types of rope
Source: https://www.drillsafe.co.za/drillsafe-articles/what-is-synthetic-rope

## Slide 16: Properties of rope
Breaking load, commonly expressed in kilogram-force, kiloNewtons (102 kgf), tonnes (1000 kgf) or pounds force – It is the minimum load under which rope breaks.
Elongation - All ropes, including wire rope, elongate when loaded. The next most important mechanical property of ropes after strength and low weight is the extent to which they stretch.

## Slide 17: Properties of rope
Fatigue- The ability to resist progressive damage from cyclic loading or long term static loading. Ropes that are cycled under load are subject to tensile fatigue.
Creep- The tendency of a material to move slowly or deform permanently under the influence of persistent mechanical stresses. Creep rupture relates to the time to fail under a given load.

## Slide 18: Rope applications
5
6
Agriculture
Fishing
Aquaculture
Shipping
Industrial
Sports.
2
1
3
4

## Slide 19
Shipping Ropes

## Slide 20: Mooring Operation

## Slide 21: Mooring Ropes

## Slide 22
Challenges – Mooring ropes
Weight of ropes should be reduced
Handling of ropes should be easier
Can the bulk be reduced??

## Slide 23
Garfil PP Hawser (1983)
Maxima Hawser (1998)
Maxiflex Hawser (2002)
Maxigold Super Hawser (2009)
Plateena Hawser (2009)
X2 Hawser (2013)
X2 Ultra & Ultima (2016)
X2 Neo (2021)
8 Strand Ropes –Evolution journey

## Slide 24
Developments in 8 Strand Shipping Ropes
Enhancing Safety in Ropes
Providing Higher Abrasion Resistance and Higher Life
Low Elongation in Ropes
X2 Range of Shipping Ropes
X10 Rope
Break Indication Rope
X2 Coated Ropes
X2 Low Elongation Rope
X2
X2 Ultra
X2 Ultima
X2 Neo
X2, X2 Ultra, X2 Ultima, X2 Neo
X10 Delayed Snapback
Break Indication (B.I.)
X2 Low Elongation
X2 Coated

## Slide 25
X2 & X2 Neo RANGE OF SHIPPING ROPES
DOWNSIZING –
  Reduction in bulk , hence improved handling and reduced fatigue
BETTER TCLL VALUE
  Longer time to retirement, higher value effectiveness
LOW SNAPBACK
  Crew Safety is most important !

## Slide 26
1. DOWNSIZING & EASE OF HANDLING
PP
76 mm
574 kg/220m
68500 kgf
Polysteel
64 mm
407 kg/220m
67500 kgf
X2
60 mm
358 kg/220m
69350 kgf
Lower Diameter of Rope
Better Strength to Weight Ratio
Better Crew efficiency
Ease of handling
Better time utilization
Less Crew Fatigue
Ease of Handling Less Mooring Time Efficiency of Vessel

## Slide 27: Strengths Comparison:
Std PP Rope 8 str |  |  | X2 (High strength PP) 8 str |  |  | X2 Neo (Highest strength PP) 8 str |  |  | X2 to std rope | X2 Neo to std rope
Dia. | Linear Density | Breaking Strength | Dia. | Linear Density | Breaking Strength | Dia. | Linear Density | Breaking Strength | BL Ratio | BL Ratio
mm | gm/mtr. | Kgf | mm | gm/mtr. | Kgf | mm | gm/mtr. | Kgf |  | 
60 | 1632 | 59500 | 56 | 1417 | 60750 | 52 | 1222 | 58685 | 118% | 132%
64 | 1850 | 67500 | 60 | 1627 | 69350 | 58 | 1520 | 71665 | 117% | 129%
74 | 2459 | 88500 | 68 | 2089 | 89200 | 66 | 1970 | 90300 | 119% | 127%
88 | 3509 | 125000 | 82 | 3038 | 127400 | 78 | 2749 | 127600 | 118% | 130%
96 | 4170 | 148000 | 90 | 3660 | 152450 | 84 | 3188 | 147070 | 117% | 130%
 |  |  |  |  |  |  |  |  | 118% | 131%

## Slide 28: Tension Fatigue Testing (TCLL Value)
Tension fatigue occurs in synthetic ropes subjected to fluctuating loads over an extended period of repeated cycles during use.
TCLL values express the maximum percentage of the breaking strength at which a rope can be cycle loaded 1,000 times.
A higher TCLL Value indicates higher resistance to cyclical tensile loading.
It results in degradation of the material and a reduction in the strength of the rope.
CYCLES FOR TCLL TESTING |  | 
 | Maxima | X2
10 - 50% Load-1000 Cycles | Completed | Completed
10 - 60% Load-1000 Cycles | Completed | Completed
10 - 70% Load-1000 Cycles | Completed | Completed
10 - 80% Load-1000 Cycles (1ST ITERATION) | Completed | Completed
10 - 80% Load-1000 Cycles (2ND ITERATION) | Broke after 138 cycles | Completed
10 - 80% Load-1000 Cycles (3RD ITERATION) | NA | Broke after 317 cycles
TCLL Values | 80.44 | 82.36

## Slide 29
2. HIGHER VALUE EFFECTIVENESS
TCLL Value highest in class
Low Yarn To Yarn Friction
Better Shock absorbance
Ability to withstand cyclic load – highest in its class –
Chart: EQUIVALENT CYCES AT 80% LOAD
| Tipto Eight | Eurofloat | Euroflex | Maxima | X2
 | 113 | 168 | 888 | 1251 | 2430
Longer Usage Life Lower Cost of Ownership Lower Operating Cost

## Slide 30: X2 Ultima (Floating Mixed Ropes)
The new technologically superior X2 Ultima ropes made from composite Fiber of high tenacity polyester & X2 yarn in a specified composition making it a floating rope.
Higher strength to weight ratio
Torque free and balanced construction
Better abrasion resistance
Chemically inert
Excellent shape and original weight retention
Excellent shock absorption capacity, Low snap-back
No loss of breaking strength in wet conditions
Retains flexibility even after prolonged use
Floating rope
Features/Benefits
Technical Specification
Material: X2 (75%) & Polyester (25%)
Construction : 8 Strand
Color : Natural White
Elongation @ Break : 18 –20%
Specific gravity : 1.0
MEG 4 complaint

## Slide 31
Comparison
Std PP Rope |  |  |  | X2 (High Strength PP) |  |  |  | X2 Ultima (High Strength Mixed PP & Polyester Rope) |  |  | 
Dia(mm) | LD(g/m) | BS(kgf) | BL(m) | Dia(mm) | LD(g/m) | BS(kgf) | BL(m) | Dia(mm) | LD(g/m) | BS(kgf) | BL(m)
64 | 1850 | 67500 | 36486 | 60 | 1627 | 69350 | 42636 | 51 | 1490 | 69300 | 46510
72 | 2341 | 84500 | 36097 | 66 | 1968 | 84000 | 42683 | 57 | 1803 | 85000 | 47144

## Slide 32
Better Ideas in Action
UHMWPE Ropes
www.garwarefibres.com

## Slide 33
UHMWPE– FEATHER LIGHT AS STRONG AS STEEL
One of strongest known synthetic fiber in the world
  As strong as steel wire of the same diameter – BUT 7 TIMES LIGHTER !!!!
  Floats on water
  Extremely durable
High Strength to weight
Light Weight
Cost of
Ownership
Safety & Ease of Handling
Increased
Life

## Slide 34
UHMWPE– FEATHER LIGHT ROPE AS STRONG AS STEEL
High Strength to weight

## Slide 35: UHMWPE Ropes
Their higher strength to weight ratio makes it easier to handle while operation over the conventional steel wire ropes.
We manufacture UHMPE ropes in 12 strand with a protective jacket.
Technical Specifications
Material: UHMPE Fiber
Construction : 12 Strand
Color : Yellow (treated)
Features / Benefits
− High Strength – Higher strength to weight ratio.
− Lower Weight – Hence easy to handle / Safe
− High Abrasion resistance
− Low elongation at break as compared to Steel Wire ropes. Weight
almost 7-8 time less.
− Excellent Chemical and UV resistance.
− Low Snap Back
− Very High TCLL Value

## Slide 36
Better Ideas in Action
Safety in Ropes
www.garwarefibres.com

## Slide 37
Shipping Ropes –
Delayed Snapback with Break Indication Rope

## Slide 38
Mooring Operation – Potentially Most Dangerous Marine Activity:
Last 20 years – 58% marine injuries during Mooring Operations
Tankers, Bulk Carriers and Tugs make 50% of Incidents
53% due to Rope Parting…!!! Snapback of mooring line causes serious injury
  1:4 chance of Leg injury or limb loss,
  1:7 chance of back injury
  1:7 chance of death
Mooring Operations - Risks
Need for Rope with enhanced safety features

## Slide 39
Solutions Offered:
To reduce the impact of Parting Mooring Rope (X10 Rope)
To help in evaluation of wear and tear in rope for right time retirement (Break Indication Rope)
Mooring Operations - Risks

## Slide 40
Specially designed rope to enhance Safety on Board!!
1. X 10 & BI Rope – Delayed Snapback Rope
X10 + BI rope will reduce probability of such accidents
On-board safety
Indicator for external wear
X10 + BI Rope
Delayed Snapback
Rope Strength
RRS Component for delayed snap back
Break Indicator for external wear and tear detection

## Slide 41
Proven by Testing at Tension Technology International (TTI), UK as per CI 1502-12
Sample before break
Sample after first break
RRS component
At loading rate of 3 mm/sec (similar to mooring condition),
Sufficient time of more than 4 minute for crew to move away when they hear a sound/spot initial breakage from the rope.
1. X 10 – Delayed Snapback Rope

## Slide 42
*Bollard Pull Test performed with propeller loading rate of around 3.5 to 4 meter per second (*This is an extreme case of high speed for a Mooring rope performed only for demonstration purpose).
Sufficient time for crew (~6 sec) to move away when they hear a sound / spot initial breakage from the rope
More confident crew during mooring operation
Prior Warning Indication Enhanced Safety
X 10 – Delayed Snapback Rope

## Slide 43
Better Ideas in Action
Towing Ropes
www.garwarefibres.com

## Slide 44: Towing Operation

## Slide 45
What could we do to enhance Towing operations ?
❑ Weight of ropes should be reduced !
❑ Handling of ropes should be easier
❑ Can the bulk be reduced??
❑ Can you enhance the movements per coil before retirement ?
❑ Can you develop a rope retirement criteria or inbuilt safety
features ?
3

## Slide 46
Better Ideas in Action
X2 Ultra ropes

## Slide 47: X2 Ultra Ropes (Sinking Mixed Rope for Towing Application)
The new technologically superior X2 Ultra ropes made from composite Fiber of high tenacity polyester & X2 yarn in a specified composition for the towing purpose.
Technical Specifications
Material: X2 (50%) & Polyester (50%)
Construction : 8 Strand
Color : Natural White
Elongation @ Break : 18 – 20 %
Specific gravity : 1.13
MEG 4 complaint
✓ Downsizing
20% REDUCTION IN ROPE BULK FOR SAME STRENGTH
▪ Easier handling for crew
▪ Reduced load on winches and capstans and thus reduced wear
▪ Better rope at same coil price
✓ Better TCLL value - Increase in operational life
▪ Class leading TCLL value
▪ TCLL cycles for X2 Ultra is more than 2.5 times Maxiflex
▪ Higher TCLL imply twice number of movements before rope retirement
✓ Lower Snapback
• Crew Safety is most important!
Features / Benefits

## Slide 48
X2 ULTRA ROPES FOR TOWING
FLEX ROPE |  |  | X2 ULTRA ROPE |  |  | % DIFF.
Dia | Wt./m | BS | Dia | Wt./m | BS | 
64 | 2.25 | 82600 | 58 | 1.84 | 83000 | 18.2
80 | 3.52 | 125500 | 72 | 2.85 | 126000 | 19.1
85 | 3.97 | 140000 | 78 | 3.35 | 145000 | 15.8
18% ADVANTAGE OVER FLEX Ropes

## Slide 49
Better Ideas in Action
HMPE Soft Shackle

## Slide 50: HMPE Soft Shackle (Alternative to the metallic shackles)
Made with HMPE, the soft shackles are a replacements of the metallic shackles and carabiners which are easy to carry and install.
Technical Specifications
Material: UHMPE Fiber
Construction : 12 Strand
Features / Benefits
− High Strength – Higher strength to weight ratio
− Lower Weight – Hence easy to handle / Safe
− Weight almost 7-8 time less.
− Excellent Chemical and UV resistance.
− Low Snap Back
− Very High TCLL Value

## Slide 51
Better Ideas in Action
Synthetic Towing Assembly

## Slide 52
Synthetic Towing Assembly
Towline
Stretcher
Pennant
Soft Shackle
Plateena NEO
(UHMPE )
X2 Ultra
Plateena NEO
(UHMPE )
Plateena NEO
(UHMPE )
A composite Fiber of high tenacity
polyester & X2 yarn with better
Their higher strength to weight
ratio makes it easier to handle
while operation over the
shock absorption capacity and low
UHMPE make shackle with
stronger & lighter compared with
steel.
snapback.
High performance fiber facilitating
highest strength , lighter weight to
withstand the towing connection
conventional steel wire ropes.
X2 Ultra
Nylon
A composite Fiber of high tenacity Conventional nylon stretcher with
polyester & X2 yarn with reduce
coil recall and better abrasion
properties.
higher elongation and shock
absorption.
4

## Slide 53
Future Developments in Shipping Rope
Better Ideas in Action

## Slide 54: To enhance Operational life in Shipping Ropes
Major Issues affecting life of rope –
1. Abrasion in rope due to contact with external surfaces
2. Degradation of rope due to bending fatigue
Notes: Wet Abrasion resistance of Nylon is very poor as compared to HDPE. This can result in holes being formed in Nylon netting.
Multifilament yarn like Nylon will have lower abrasion and cut resistance due to filamentation, which breaks the individual filaments during abrasion

## Slide 55: Bending Fatigue in rope
Bending Fatigue is induced when the rope under tension is bent and cycled over the rotatable curved surface.
It plays a considerable role in deciding the life and performance of rope especially when used over winches/pulleys/sheaves
Bending Fatigue Tests covered in MEG4, Cordage Institute and DNV standards
Notes: Wet Abrasion resistance of Nylon is very poor as compared to HDPE. This can result in holes being formed in Nylon netting.
Multifilament yarn like Nylon will have lower abrasion and cut resistance due to filamentation, which breaks the individual filaments during abrasion

## Slide 56: X15 Ropes
Working on Next generation Rope Development with significant improvement in
Abrasion Resistance of rope – 50% improvement over X2
Bending Fatigue of rope – 100% improvement over X2
Chart: Cycles to failure (Abrasion Resistance)
| Maxima | X2 | X-15
Abrasion outside
Cycles to failure | 1 | 1.4797 | 2.0386
Chart: % improvement in Bending fatigue resistance
| X2 | X15
 | 100 | 215
*Normalized to a scale of 100 for X2

## Slide 57: Renew Ropes
Features | Benefits
Sustainability | Ropes made from 100% Recycled Products
Strength | No compromise, Same strength as Maxima Ropes (Danline type of ropes)
Fatigue Properties | Same as Maxima Ropes (Danline type of ropes)
Abrasion Properties | Similar as Maxima Ropes (Danline type of ropes)
Spliceability | Easily spliceable
Colour | Available in Black colour
Type | Available in both 8 strand and 3 strand

## Slide 58
Thank You